IRG/WP 12-10784

THE INTERNATIONAL RESEARCH GROUP ON WOOD PROTECTION

Section Y VVVVVVVVVV

Coconut lumber for wood decks (Cocos nucifera L.):

decay resistance against Basidiomycetes fungi

Benoit Jourez1, Cecile Verheyen1, Joris Van Acker2

1 Laboratory of Wood Technology, Direction of Forest Environment,

Department of Natural and Agricultural Environment Studies, Public Service of Wallonia

23 Av. Maréchal Juin

5030 Gembloux, Belgium

2 Laboratory of Wood Technology, Ghent University

Department of Forest and Water Management, Faculty of Bioscience Engineering

Coupure Links 653

9000 Ghent, Belgium

Paper prepared for the 43rd Annual Meeting

Kuala Lumpur, Malaysia

6-10 May 2011

Disclaimer

The opinions expressed in this document are those of the author(s) and

are not necessarily the opinions or policy of the IRG Organization.

IRG SECRETARIAT

Box 5609 SE-114 86

Stockholm Sweden

www.irg-wp.com

Coconut lumber for wood decks (Cocos nucifera L.):

decay resistance against Basidiomycetes fungi

Benoit Jourez1, Cecile Verheyen1, Joris Van Acker2

1 Laboratory of Wood Technology, Direction of Forest Environment, Department of Natural and Agricultural Environment Studies, Public Service of Wallonia, 23 Av. Maréchal Juin, 5030 Gembloux, Belgium

2 Laboratory of Wood Technology, Ghent University, Department of Forest and Water Management, Faculty of Bioscience Engineering, Coupure Links 653, 9000 Ghent, Belgium

Abstract

Since a couple of years, manufactured products of coconut wood for outdoor uses like wood decks have been proposed on the European market. These are presented as an alternative for traditional tropical timbers. In the past, coconut wood was neglected and burned for sanitary reasons and lack of interest at industrial scale. Plantation coconut trees at end of production of copra constitute a renewable resource with high added value. In order to convince the markets, natural durability for outdoor use, without preservative treatment, against wood destroying fungi characteristic of northern temperate regions is a major property that has to be checked.

Natural durability of coconut lumber was tested in the laboratory according to the European standard EN 15083-1 against brown (Coniophora puteana) and white (Coriolus versicolor) rot decay basidiomycetes fungi. Beech wood specimens were used as virulence controls. Mass losses were determined after 16 weeks exposure.

The results showed that tested coconut wood is very resistant to the brown rot fungus Coniophora puteana and resistant to the white rot fungus Coriolus versicolor. Mass loss and density of tested samples with C. versicolor are inversely related. In addition, the density shows a large variability in the test sample, more than 500 kg / m³.

These results confirm that after a selection on density criteria, the natural durability of Coconut lumber is sufficient for outdoor application in use class 3 (based on European standard EN 335 and in line with EN 460).

Key words: Coconut wood, decay resistance, durability, Coriolus versicolor, Coniophora puteana, decay fungi, wood decks,

Introduction

The coconut logs (Cocos nucifera L.) based on the agricultural crop for copra production can be harvested from plantations at an age of over 60-70 years corresponding at the end of production. They represent as such a potentially important renewable resource of wood for the producing countries (Amartey & al., 2006;Hass & Wilson, 1985; Arancon, 1997 & 2009; Jermer & al., 2011; Killmann & Fink, 1996; Peek, 1994). They provide a raw material for timber industry likely to be converted into high-value manufactured products, with a low environmental impact.

This has led in the second half of the 20th Century to the establishment of international research projects focused on the use and valorisation of coconut wood. Through these projects, many aspects were studied: wood anatomy, physical, mechanical, chemical, energy and natural durability properties, costs. The industrial valorisation of wood was also investigated: logging, wood uses, processing, impregnation, conditioning, poles, particle board, floors, saws, furniture, energy resources, charcoal, market research (Hass & Wilson, 1985; Arancon, 1997; Killmann & Fink, 1996).

Initially considered as an alternative source of wood supply to meet needs in local markets (Amartey, 2006; Arancon, 1997; Okai, 2004; Yudodibroto, 1980), manufactured products are now penetrating the markets of Western industrialised countries. This can be explained by the significant growth in demand for tropical timber in conjunction with an awareness of the importance to reduce pressure on tropical forests (Amartey & al., 2006; Arancon, 1997; Wong & al., 2005). Like other species e.g. Robinia pseudoacacia (Pollet & al., 2008), coconut could be an alternative to the use of traditional tropical timbers.

Nevertheless, the first attempts of introduction on the industrialised countries’ markets hadn’t obtained the expected success by lack of fit with the requirements of these markets (Killmann & Fink, 1996; Peek, 1994a). Recent technical solutions can solve the problems of implementation encountered in the past (Arancon, 2009).

Today, coconut floor strips are available on the European market but also in America and Australia. This represents a high added value product (Arancon, 2009). Nevertheless, in order to establish this new product on the market complementarily to the tropical timbers traditionally used , queries about some properties must be clarified: physical, mechanical and durability against wood destroying fungi characteristic of Northern temperate regions (Amartey & Hanson, 2002; Amartey & al 2006, Baillieres & al., 2010). For use as exterior decking, its natural durability has to be suitable (class 1 or 2) which allows uses in hazard classes 3 and 4. Moreover, producers must guarantee a sustainable, quality and homogeneous supply (Baillieres & al., 2010; Hass & Wilson, 1985).

The maximum diameter at the bottom of the coconut palm stem is around 30 cm (Hass & Wilson, 1985; Killmann & Fink, 1996). Average tree heights range between 15 to 20 meters but only the 2/3 of the stem can be used as constructional material, the wood from the top and centre of the trunk being too light. The wood density varies from the central part of the trunk to the external part between approximately 200 to 1170 kg/m³ (Bailleres & al., 2010; Peek 1994a; Yudodibroto, 1980). In mature coconut palm stem, three classes of wood density being high density > 600kg/m³, medium density between 400 and 600 kg/m³, and low density < 400 kg/m³, are recognised according to the position of the timber into the stem (Arancon, 2009; Killmann & Fink, 1996). The same authors conclude that low density wood does not achieve sufficient strength values and surface qualities for manufactured wooden products. Visual distinction between these classes is possible by an experienced operator by looking on the cross section for the amount of vascular bundles (Baillieres & al., 2010). In a recent publication from the Australian Government, the limits of the 3 classes have been increased by 100 kg/m³ (Bailleres & al., 2010). Moisture content increases from the bottom periphery (50%) to stem centre at the top (400%). Radial and tangential shrinkages show no significant difference (Hass & Wilson, 1985; Arancon, 1997; Killmann & Fink, 1996). The average modulus of elasticity (MOE), modulus of rupture (MOR) and compression strength of coconut wood measured on clear wood specimens at 12% are 12772 N/mm², 106 N/mm² and 69 N/mm² respectively (Arancon, 1997; Okai 2004). These values decrease from bottom to the top of the trunk. Such values concern wood at the periphery of the stem with a density above 600 kg/m³ and are comparable to those obtained with other tropical timber generally used for furniture, flooring, door and window, agricultural implements, general construction, etc. The Janka hardness for the high density class reaches about 10800 N at 12%, approximately twice higher than European oak.

Only a density higher than 600 kg/m³ (700 kg/m³ following Australian recommendations) allows application in flooring but for exterior uses natural durability must be considered too.

Coconut wood is classified as non-durable (Hass & Wilson, 1985). Under tropical conditions, its durability against wood destroying fungi is low (few months for the central part of the stem and only two and a half years for the periphery wood). In indoor conditions, only low density class should be treated against insects. For outdoor utilisation, a chemical wood protection is generally required for all density classes (Hass & Wilson, 1985; Killmann & Fink, 1996; Peek, 1994a & b). Under Northern temperate climate, resistance against wood destroying fungi seems better but wood density must be taken into account when selecting pieces for external uses. In laboratory test, the white and brown rot fungi (basidiomycetes) are able to damage severely the coconut wood and observed mass losses are inversely proportional to the density (Peek, 1994a). The same author classified the high density coconut wood as non-resistant against the white rot fungus (Coriolus versicolor) and resistant against brown rot fungi. He concluded that coconut wood cannot be recommended for exterior uses without prior preservative treatment. Different authors make the same observation (Arancon, 1997; Killmann & Fink, 1996).

The aim of this study was to determine the natural durability against brown (Coniophora puteana) and white (Coriolus versicolor) rot decay basidiomycetes fungi characteristic of northern temperate regions of coconut floor strips imported from Malaysia according to the European standard procedure CEN/TS 15083-1. These planks are destined for exterior decking.

Material and methods

Untreated coconut wood (Cocos nucifera L.) floor strips were supplied by a Belgian import company. This material was produced by a Malaysian manufacturer and warranted with a density higher than 900 kg/m³. Test specimens (1.5 x 2.5 x 5 cm) were cut from 28 planks (20 x 90 x 2000 mm) selected at random from a batch of 800 planks and stocked in climatic room (20 ( 2)°C and (65 ( 5)% relative humidity. Two specimens per plank were tested for each fungus and 3 specimens per plank were used to determine humidity and density. Beech wood (Fagus sylvatica L.) was used as reference specimens for virulence control.

Humidity of reference specimens and test specimens was respectively 10,0% and 12,9% before exposure to fungal attack.

The fungi used in the experimentation were Coniophora puteana (Schumacker ex Fries) Karsten (BAM Ebw. 15) as brown rot fungus and Coriolus versicolor (Linnaeus) Quélet (CTB 863A) as white rot fungus.

The test was performed according to  the European standard procedure CEN/TS 15083-1 (2005) “Durability of wood and wood-based products – Determination of the natural durability of solid wood against wood-destroying fungi, test methods – Part 1: Basidiomycetes”. After conditioning at (20 ( 2)°C and (65 ( 5)% relative humidity, test specimens and reference specimens, were introduced aseptically in Kolle flasks on a malt agar culture medium previously inoculated with fungus. The flasks were stored for 16 weeks in a climatic room under standard conditions (20 ( 2)°C and (65 ( 5)% relative humidity. At the end of the exposure time, mass losses were determined and natural durability of tested coconuts wood classified according to CEN/TS 15083-1 (2005) annex D.

Results and discussion

The fungal activity of the two fungi tested on beech reference specimens reached the minimum required by the standard. The mean mass losses obtained were 30.2% and 38.0% respectively for Coniophora and Coriolus after 16 weeks.

At the end of the exposure time (16 weeks), the mass loss for each coconut test specimen was calculated. Median value for all test specimens exposed to each test fungus and durability class against wood-destroying basidiomycetes fungi were determined (table 1). The mean final moisture contents of the test specimens were 43.4% and 49.4% respectively for Coniophora and Coriolus.

Table 1. Median mass loss and natural durability class of coconut wood against basidiomycetes fungi.

| Basidiomycetes fungi | Median mass loss | Durability class | Description |
| --- | --- | --- | --- |
| Coniophora puteana | 0.00 | 1 | Very durable |
| Coriolus versicolor | 5.62 | 2 | Durable |

The Coriolus versicolor showed a higher decay level than the Coniophora puteana and lead to classify coconut wood in durability class 2 (Durable). The obtained mass losses analysed according to EN 350-1 lead to same durability classes. These results allow the use of coconut floor strips in outdoor condition without prior preservative treatment according to the specifications of EN 460 “Durability of wood and wood-based products – Natural durability of solid wood – Guide to the durability requirements for wood to be used in hazard classes”. Results obtained with Coniophora puteana are similar to those obtain by Peek (1994a) on Indonesian coconut trees. On the other hand, results obtained with Coriolus versicolor are not consistent with those of Peek who declared the coconut wood of high density class (> 600 kg/m³) as non-resistant against white rot fungus. Several authors conclude that coconut wood cannot be recommended for exterior use without prior preservative treatment (Arancon, 1997; Killmann & Fink, 1996; Peek, 1994a). A lower minimum density of test specimens can probably explain the contradiction with the results obtained in this study.

The information contained in this paper applies only to the sample of timber tested. Actually, the tested planks were selected to suit outdoor decks without chemical treatment. Inside a coconut log, depending on radial and longitudinal position, important density variations exist (Peek, 1994a). It is therefore possible in a single plank to find areas of different density because localised higher or more inwardly into the stem in function of cutting pattern (Baillieres & al, 2010; Hass & Wilson, 1985; Killmann & Fink, 1996). Despite a selection of planks with a density criterion above 900 kg/m³, 25% of the sawn test specimens showed lower values. The density of 200 test specimens was 990 ( 116 kg/m³ and ranked between 702 and 1205 kg/m³. Mean volume of the specimens was determined by hydrostatic method. The average humidity at the time of measurement was 12.9%.

Natural durability varies widely inside a stem according to the density class considered, even if other factors can be involved (Hass & Wilson, 1985; Peek, 1994a). The relationship between density and mass loss supports the idea of a strict selection necessity. In Figure 1, it appears clearly that a density higher than 900 kg/m³ ensures a mass loss under 10%. Below this critical density the test specimens with higher mass losses were observed after being in contact with the Coriolus.  Using the assessment approach as proposed by Van Acker et al. (2010) a considerable service life can be expected from this material since no specimens showed mass losses higher than 10 %. The Weibull distribution derived from the data on decay by Coriolus clearly show that the selection of material with a density of over 900 kg/m³ (here on individual specimens) allows for a very critical appraisal of durability class D2 (Figure 2, sapelli used for benchmarking).

Figure 1: Mass loss due to Basidiomycetes fungi versus density

| Wood species | Fungus | Med(X) | r0,1 | r0,9 | %D1 | %D2 | %D3 | %D4 | %D5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Coconut | COR | 5.3 | 2.9 | 7.9 | 43.2 | 56.0 | 0.8 | 0.0 | 0.0 |
| Sapelli |  | 20.1 | 11.8 | 28.2 | 0.5 | 5.1 | 16.1 | 72.7 | 5.6 |

Figure 2: Weibull distributions of mass loss by Coriolus versicolor (%, x-axis) and durability of coconut (Cocos nucifera) and sapelli (Entandrophragma cylindricum)

Conclusions

Natural durability of coconut wood floor strips for exterior use, imported from Malaysia, and selected on density at > 900 kg/m³, was tested with white and brown rot fungi following European standard procedure CEN/TS 15083-1 (2005).

The coconut wood with a median mass loss of 6%, was classified as durable (class 2) when exposed to the white rot fungus Coriolus versicolor. Brown rot fungus Coniophora puteana proved ineffective, median mass loss was close to 0%.

The results obtained in this experimentation were better than those obtained previously by other authors. The reason given for better behaviour can be explained by the higher wood density values measured in this experiment. The average wood density of test specimens was 990 kg/m³.

The selection criterion based on a density greater than 900 kg/m³ and the planks selection work ensure a class 2 of durability compatible with outdoor uses in temperate Northern regions.

Confirmation of these results with other sources of wood is needed. In addition, exporters will have to be able to guarantee a sustainable, homogenous and quality supply.

Acknowledgements

The authors wish to thank the Public Service of Wallonia and the LIME Alternative Supplier SPRL for their financial support. They warmly acknowledge Alain Vandersteen (DEMNA), as well as Lahcen Hadiy and Pascal Thibaut (GxABT) for their valuable technical assistance.

References

Amartey S.A., Hanson F.R. (2002) Natural decay resistance of some lesser-used tropical hardwoods from Ghana. Intern. Res. Group. on Wood Preserv. (IRG), Doc No. IRG/WP/02-10438, 11pp.

Amartey S.A., Humar M., Donkor B., Pohleven F. (2006) Decay resistance of coconut and rubber woods Alternative wood species from Ghana. Intern. Res. Group. on Wood Preserv. (IRG), Doc No. IRG/WP/06-10596, 7pp.

Arancon R.N. (1997) Focus on coconut wood. Asia-Pacific forestry sector outlook study, working paper N° APFSOS/WP/23, 36pp.

Arancon R.N. (2009) The situation and prospects for the utilization of coconut wood in Asia and the Pacific. Asia-Pacific forestry sector outlook study II, working paper N° APFSOS II/WP/2009/15, 45pp.

Baillieres H., Hopewell G., House S., Redman A., Francis L., Fehrmann J. (2010) Cocowood processing manual. From coconut wood to quality flooring. Department of Employment, Economic Development and Innovation, Brisbane,44pp.

CEN/TS 15083-1 (2005) Durability of wood and wood-based products – Determination of the natural durability of solid wood against wood-destroying fungi, test methods – Part 1: Basidiomycetes, 20pp.

EN 335-1 (2006) Durability of wood and wood-based products. Definitions of use classes. General, 14pp.

EN 350-1 (1994) Durability of wood and wood-based products – Natural durability of solid wood – Part 1: Guide to the principles of testing and classification of the natural durability of wood, 16pp.

EN 460 (1994) Durability of wood and wood-based products – Natural durability of solid wood – Guide to the durability requirements for wood to be used in hazard classes, 9pp.

CEN/TS 15083-1 (2006) Durability of wood and wood-based products – Determination of the natural durability of solid wood against wood destroying fungi, test methods – Part 1 Basidiomycetes, 20pp.

Haas A., Wilson L. (1985) Coconut wood: Processing and use. Food And Agriculture Organization Of The United Nations, ISBN 92-5-102253-4, 68pp.

Jermer J., Wong A., Segerholm K., Nilsson T. (2011) Durability testing of coconut shell according to ENV 807. Intern. Res. Group. on Wood Preserv. (IRG), Doc No. IRG/WP/11-10761, 8pp.

Killmann W., Fink D. (1996) Coconut palm stem processing: Technical handbook. Protrade, Deutsche Gesellschaft für Technische Zusammenarbeit (GTZ) GmbH Dag-Hammarskjöld-Weg 1–5 D-65760 Eschborn, http://www.fao.org/docrep/009/ag335e/AG335E00.htm#pro .

Okai R., Frimpong-Mensah K., Osei Kwarteng J., Arthur S. (2004) Characterisation of mechanical strength properties of coconut wood infested with the Cap St Paul Wilt disease. Holz Roh Werkst 62: 390-392.

Peek R-D. (1994a) Utilization of Coconut Timber from North Sulawesi, Indonesia. Part 1 Durability. Intern. Res. Group. on Wood Preserv. (IRG), Doc No. IRG/WP/94-30044, 11pp.

Peek R-D. (1994b) Utilization of Coconut Timber from North Sulawesi, Indonesia. Part 2 Treatability. Intern. Res. Group. on Wood Preserv. (IRG), Doc No. IRG/WP/94-40025, 15pp.

Pollet C., Jourez B., Hebert J. (2008) Natural durability of Black locust (Robinia pseudoacacia L.) wood grown in Wallonia, Belgium. Can. J. For. Res. 38: 1366-1372.

Van Acker, J., Van den Bulcke, J., De Boever, L. (2010). The biological durability approach for wood product performance and service life prediction. Intern. Res. Group on Wood Prot., Document IRG/WP10-20457, 22 p.

Wong A.H.H., Kim Y.S., Singh A.P., Ling W.C. (2005) Natural durability of tropical species with emphasis on Malaysian hardwoods – Variations and prospects. Intern. Res. Group. on Wood Preserv. (IRG), Doc No. IRG/WP/05-10568, 33pp.

Yudodibroto H. (1980) The potential use of impregnated coconut wood for power line poles in rural areas of Java. Intern. Res. Group. on Wood Preserv. (IRG), Doc No. IRG/WP/3130, 8pp.