## Slide 1
Development and optimization of pegylated lipoplexes for vaginal application
Lechanteur Anna
SF Nano Workshop - Porto - 03rd October 2014

## Slide 2
Human PapillomaVirus: HPV
Normal cervix
LSIL
HSIL
Invasive cancer
Surgery
Chemotherapy
Radiation
15 years
CERVICAL CANCER:
World Health Organization (WHO)
Fourth cause of cancer death among women
266000 deaths in 2012

## Slide 3
E6 and E7 oncoproteins
 E6 and E7 oncoproteins
Doorbar, J. Molecular biology of human papillomavirus infection and cervical cancer. Clinical Science. 2006. 110, 525–541

## Slide 4
E6 and E7 oncoproteins
E6 and E7 oncoproteins :
 interesting targets
 appropriate for siRNA therapy
 E6 and E7 oncoproteins

## Slide 5
Strategy
 siRNA anti-E6
 siRNA anti-E7
 siRNA anti-E6 + siRNA anti-E7
siRNA

## Slide 6
Validation of siRNA anti-E6/E7 efficiency
 Evaluate different siRNA combinations with Oligofectamine® in order to induce apoptosis on CaSki cells (HPV16 + cells)
SCR
E7
Transfection time: 3 days

## Slide 7
Objectives
Cationic lipid: DOTAP
Cholesterol
Fusogenic lipid: DOPE
DOTAP/Chol/DOPE
1/0,75/0,5
+ siRNA E6 100nM
N/P ratio = 2,5

## Slide 8
Objectives
MPP
Avoid electrostatic adhesive interaction
Avoid hydrophobic entrapment
Uncharged hydrophilic polymer
DSPE-PEG 750 and DSPE-PEG 2000
Low drug doses
Site specific delivery
Low systemic side effects
Circumvention of first-pass hepatic clearance
Vaginal route
S.K. Lai et al. / Advanced Drug Delivery Reviews 61 (2009) 158–171

## Slide 9
Objectives
4) Western Blot
Physicochemical assays
- Z-average size - PdI
- Zeta potential
- Percentage of encapsulation
3) qRT-PCR
- Flow cytometry
- Confocal microscopy

## Slide 10
Liposome
Lipoplexes (N/P 2,5)
siRNA (100nM)
+
Seeded CaSki cells in 6-wells plate
D 0
Transfection
D 1
D 2
Flow cytometry / Confocal microscopy
qRT-PCR /
Western Blot
D-1
General methods
+
DSPE-PEG 750

or
DSPE-PEG 2000
Lipoplexes formulation
In vitro assays
10%
30%
50%

## Slide 11
Physicochemical properties
Size and Zeta potential measurements (Malvern NanoZS)
Encapsulation of siRNA onto liposomes
(Ribogreen®)

## Slide 12
In vitro efficiency
CaSki cells (HPV16 +)
[siRNA-scramble FITC] = 100nM
Oligofectamine® 6µL
Lipoplexes N/P 2,5
n=3
Evaluation of transfection potential by flow cytometry assay (FACS Canto II)
Notes: Mettre si seul

## Slide 13
In vitro efficiency
Evaluation of transfection potential by confocal microscopy (Leica SP5)
Lipoplexe- siRNA FITC 100nM
Lipoplexe PEG2000 50%- siRNA FITC
siRNA FITC 100nM
Blue: Nucleus staining with DAPI
Green: siRNA FITC
Objective: 63x
Pinhole: 309,95
Empty liposome
Notes: Mettre si seul

## Slide 14
In vitro efficiency
Evaluation of releasing potential of siRNA E6 into the cytoplasm by qRT-PCR
CaSki cells (HPV16 +)
[siRNA-scramble and E6] = 100nM
Oligofectamine® 6µL
Lipoplexes N/P 2,5
Normalization: GAPDH primers
n=3

## Slide 15
In vitro efficiency
CaSki cells (HPV16 +)
[siRNA-scramble and E6] = 100nM
Oligofectamine® 6µL
Lipoplexes N/P 2,5
Evaluation of p53 re-expression by Western Blot

## Slide 16
Cytotoxicity assay (WST-1)
CaSki cells (HPV16 +)
[siRNA-scramble] = 100nM
Oligofectamine® 6µL
Lipoplexes N/P 2,5
n=4
In vitro efficiency

## Slide 17
Lechanteur A, Furst T et al, siRNA encapsulation into liposomes for a topical treatment of cervical preneoplastic lesions: promising gene delivery system, 2014, Submitted
Conclusion
Appropriate physicochemical properties
High transfection and MFI
mRNA E6 extinction
p53 re-expression

## Slide 18
 Confirm the hypothesis: siRNA are blocked in the endosome by co localization of Alexa546-siRNA and NDB-cholesterol (confocal microscopy) and LysoTracker® probe
 Increase proportion of fusogenic lipid = DOPE
 Perform apoptosis and proliferation assay
Prospects
Lechanteur A, Furst T et al, siRNA encapsulation into liposomes for a topical treatment of cervical preneoplastic lesions: promising gene delivery system, 2014, Submitted

## Slide 19
Acknowledgements
EVRARD Brigitte
PIEL Géraldine
FURST Tania
FRERE Antoine
PALAZZO Claudio
ALVAREZ Maria-Luz
Laboratory of Experimental Pathology
DELVENNE Philippe
HUBERT Pascale
HERFS Michael
DEMOULIN Stéphanie
RONCARATI Patrick
Promotors: Géraldine PIEL (LTPB) and Pascale HUBERT (LEP)
GIGA-Imagerie et Cytométrie de flux
ORMENESE Sandra
STEPHAN Rafaat
University of Angers
KANBER Erdem