## Slide 1: Quasicontinuum analysis of interaction between screw dislocation and coherent twin boundary
TRAN Hoang-Son
HAREESH Tummala
DUCHENE Laurent
FIVEL Marc
HABRAKEN Anne Marie
7 Septembre 2016
University of Liège
PAI Intemate P7/21

## Slide 2
Introduction
1. Interaction screw dislocation – CTB
Outline ²
2. Triple Junction
3. Conclusion & Perspectives
2

## Slide 3
Introduction ²
3
Hanriot1993
Fivel 2008
Willems 2005
Ludwig et al 2009
100µm
Tran 2013
Micro
Macro
Embouti Cruciforme projet européen CashForm 2000
DM, Berbenni 2013

## Slide 4
Why are Grain Boundaries (GB) so important?
GB vary a great deal in their characteristics (energy, mobility, chemistry)
Many properties of a material - and its microstructural evolution - depend on the nature of GB.
Type of GB good or bad corrosion properties, mechanical properties (creep)
Some GBs : good atomic fit  resistant to sliding, low diffusion rates, low energy, etc.
Bicrystal interface energy for copper and aluminum tilt [1-10] interface models (Tschopp, M.A. 2008)
Coherent Twin Boundary studied
Introduction ²

## Slide 5
Transmission of screw dislocation through the Σ3 boundary in Cu (Pestman et al. 1991)
Absorption of the screw dislocation in the boundary plane into two g.b.d.s in static simulation
Introduction ²

## Slide 6
The reaction modes between screw dislocation and CTB (Jin et al. 2006 )
The reaction modes between screw dislocation and CTB (Zheng et al. 2009)
Introduction ²

## Slide 7
Interaction of the lattice dislocations with a Σ=11 by QC (Wenshan et al. 2014)
Interactions Between Dislocations and GB by QC
Introduction ²

## Slide 8
x
y
z
Atomistic zones
Interaction between atoms based on Embedded atom theory (EAM)
FEM zonesCauchy-Born rule:
atoms mapped according to a continuum deformation field
+
Access to the core contribution
Degrees of freedom judiciously reduced
-
No Temperature effect (0K potentials)
No Strain-rate effect (quasi-static)
2D only
Still a size limit for polycrystalline structures
Quasicontinum method provides to DDD :
Grain Boundary –Dislocation interaction mechanisms
Variation of Energy
Critical stress (generation, transmission..)
(1)
(2)
(3)
(4)
slip systems have the same Burgers vectors
slip systems have different Burgers vectors (leaving a residual boundary dislocations)
slip systems have different Burgers vector (leaving a residual boundary dislocations)
the grain boundary acts as an impenetrable boundary,
Direct transmission
Indirect transmission
No transmission
Introduction ²
Notes: We apply the Quasi-Continuum Method (QCM) developed by Tadmor and co-workers to study the nucleation of dislocation and the interaction between dislocation and CTB coherent twin boundary in copper.
The QCM is a molecular static technique which find the solution of equilibrium atomic configurations by energy minimization, for external loads or displacements.
The problem is modeled without explicitly representing all the atoms in the cell; here the regions of small deformation gradients are treated as a continuum media by the finite element method
The key advantage of QC code is the automatic adaptation to ensure full atomistic resolution when dislocations are emitted as well as at the interactions between the dislocations and the grain boundaries
Here , i represent four main mechanism of interaction between dislocation and grain boundary.
  There are two possibilities of direct transmission, indirect transmission an no transmission occur

## Slide 9
Orientation relation and several slip systems between a twin GB
and the matrix (Thompson tetrahedron). The CTB plane is defined as the (1 1 1) CBA plane
y1
x1
z1
D
B
A
C
D’
γ
δ
Plane of QC
Grain1
Grain2
γ'
Plane of TB
P
H1
H2
d
Indenter
x1
y1
z1
x2
y2
z2
Grain 1
Grain 2
Twin boundary
Orientation Grain 1 : X[-1-12], Y[111], Z[-110]
Grain 2 : X[ 1 1-2], Y[111], Z[1-10]
x
y
z
Quasicontinuum model

## Slide 10
Twin boundary
Orientation Grain 1 : X[-1-12], Y[111], Z[-110]
Grain 2 : X[ 1 1-2], Y[111], Z[1-10]
x
y
z
P
H1
H2
d
Indenter
x1
y1
z1
x2
y2
z2
Grain 1
Grain 2
Coherent Twin Boundary structure (CTB)
Grain1
Quasicontinuum model
Grain2

## Slide 11
Orientation Grain 1 : X[-1-12], Y[111], Z[-110]
Grain 2 : X[ 1 1-2], Y[111], Z[1-10]
Twin boundary Σ3 {111l}
Orientation relation and several slip systems between a twin
and the matrix (extended-Thompson tetrahedron). The CTB plane is defined as the (1 1 1) CBA plane
y1
x1
z1
D
C
γ
δ
Plane of QC
Grain1
Grain2
γ'
Plane of TB
Q
D
C
b -plane of (-110)
a -plane of (-110)
B
B
A
y1
x1
z1
Quasicontinuum model

## Slide 12
1.Interactions Between Screw Dislocations and Coherent GB
Nucleation of screw dislocation
whole system with domain partition
CSD parameter
Out of plane displacement field

## Slide 13
x
y
z
Distributions of the virial shear stress σyz near CTB
1.Interactions Between Dislocations and Coherent TB by QC

## Slide 14
1.Interactions Between Screw Dislocations and Coherent GB
Macroscopic view of transmission
(Energy field)
Schematic of screw dislocation – twin interactions
Detailed mechanism of transmission
x
y
z

## Slide 15
Ref | Material/T° | EAM/Mechanism | CRSS | Force Dislo/GB
(Pestman et al. 1991) | Cu/0K/ | Finis-Sinclair /Transmission/FE | 1500 MPa | 500 MPa
(Jin et al. 2006) | Al/10K Cu/10K | Mishin/Absortion/FE Mishin/Transmission/FE | 100 MPa 465-510 MPa | 100 MPa 300 MPa
(Chen et al. 2007) | Al/ Cu | Mishin/Absortion Mishin/Transmission/FE |  | 140MPa (Al) 220MPa(Cu)
(Dewald and Curtin 2007) | Al | Ecolessi-Adams Absortion/F |  | 
(Zhu et al. 2007) | Cu | Mishin/ 1st path Absorption-Desorption/FE 2nd path Transmission/F |  | 
(Zheng et al. 2009) | Cu/300K | Daw-Baskes-Mishin/ 1st Transmission/F 2nd Absortion/FE | No infos | No infos
(Chassagne et al. 2011) | Cu/300K | Mendelev/Transmision/FE Ackland/Transmission/FE Foiles/Transmission/FE | 510 MPa 540 MPa 460 MPa | 400 MPa 400 MPa 400 MPa
(Wei and Wei 2012) | Cu/0.1K | Mishin/Absortion/FE | 288.2 MPa | 288.2MPa
1.Interactions Between Dislocations and Coherent TB by QC

## Slide 16
Interaction of the lattice dislocations with a Σ=3 {111} (Sangid et al. 2007)
Idea of control box
1.Interactions Between Dislocations and Coherent TB by QC

## Slide 17
1.Interactions Between Screw Dislocations and Coherent GB
Local stress evolution in control box at the interaction zone (virial stress)
Control box
Critical shear stress (608 MPa)

## Slide 18
1.Interactions Between Dislocations and Coherent TB by QC
Dislocation Dynamics Algorithm (Bi-crystal)
Bi-crystal microstructure
Dislocation microstructure
Dislocation loops; Realistic microstructures
Artificially pinned Frank-Read sources
Crystal number
X-, Y- and Z- coordinates
Burgers vector (b)  [TT]
Glide direction (l)  [TT]
Crystal parameters (position, dimensions, orientation)
Grain boundary → Frame of reference
Real/lab ↔ Crystal/local
Dislocation Dynamics loop
Procedures followed at every time step ()
Segments
Stress-field
Mobility law
Plastic strain
Planar defects
Linear defects
Twin boundary
Disorientation ()
Low Angle Grain Boundary
High Angle Grain Boundary
Procedure  Resultant Burgers vector (RBV)
Annihilation
Hirth, Lomer
Collinear interaction
Pileup
Cross-slip
Edge + Screw
Edge (b perp l); Screw (b || l)
Elastic isotropy
Fpk= σ.n.b

## Slide 19
Dislocation transmission across CTB by DDD simulation
1.Interactions Between Dislocations and Coherent TB by QC

## Slide 20
1.Interactions Between Screw Dislocations and Coherent GB
Schematic illustration of dislocation pile-up at a grain boundary
The Peach –Kohler force vanish at each point throughout the pile up in equilibrium
Condition can be represented by an the continuum theory
Dislocation density function
Number of dislocation N
Transmission stress
(Hirth and Lothe 1982)
Hall-Petch type law

## Slide 21
1.Interactions Between Dislocations and Coherent TB by QC
High density of dislocation near Grain Boundary before transmission

## Slide 22
Schematic illustration of dislocation pile-up at a grain boundary
The Peach –Kohler force vanish at each point throughout the pile up in equilibrium
Condition can be represented by an the continuum theory
Dislocation density function
Number of dislocations
activation stress of source
Yield stress
Improved link with DDD
1.Interactions Between Dislocations and Coherent TB by QC
Force on the leading dislocation

## Slide 23
Schematic illustration of dislocation pile-up at a grain boundary
1.Interactions Between Dislocations and Coherent TB by QC
(Chakravarthy and Curtin, 2010)

## Slide 24
In Cu (Chassagne et al. 2011)
In Cu-4.5% Al (Swann and Nutting, 1961)
Transmission electron micrograph of a dislocations a pile up
Dislocation source
Transmission of dislocation by high stress concentration
1.Interactions Between Screw Dislocations and Coherent GB
Notes: Discussion
In Figure, transmission has not occurred (8 dislocation in the pile-ups), at this scale ( > 200nm) , the Figure indicated that at least 10 dislocation is necessary for the first transmission occurred.
On a larger scale in Figure needs more number of dislocation to initiate a transmission.

## Slide 25
Schematic illustration of dislocation pile-up at a grain boundary
Number of dislocation in pile up before transmission
1.Interactions Between Dislocations and Coherent TB by QC
Classic model
New model
DDD results
Classic model
New model

## Slide 26
Schematic illustration of dislocation pile-up at a grain boundary
2.Interactions Between Screw Dislocations and Coherent GB
(Delincé, M. et al. 2007)
w length of dislocation arrangement

## Slide 27
Schematic illustration of dislocation pile-up at a grain boundary
1.Interactions Between Screw Dislocations and Coherent GB
Lsource=0.25D
Lsource=0.1D
Distribution of density of dislocation

## Slide 28
2.Triple Junction by QC
U
L
H
x1
y1
z1
x2
y2
z2
Grain boundary
Grain 1
Grain 2
x3
y3
z3
α2
α1
α3
Σ12
Σ13
Σ23
Grain 3
Σ12 = 9
Σ23 = 27
Σ13 = 3
α1 = 163.14
α2 = 125.10
α3 = 71.76
H=164
L=160
Σ1 Σ2 = d2 Σ3
with d = 1 or 3
Schematic representation of tricrystal model
Atomic structure projected onto the x-y plane
Interfaces structures and Structural Unit Model (SUM) notation for [1-10] interface models

## Slide 29
3.Triple Junction by QC
Global view centro symmetric deviation parameter map
Nucleation of dislocations at TJ and GB
Atom shuffling at GB
Atomic configuration is stable

## Slide 30
5. Conclusion and perspective
Simulation results by QC in line with full MD simulation
CTB is a strong barrier to slip transmission
Highlight the interaction mechanism of dislocation and CTB
Quantitative estimation of local critical stress for transmission
Provide mechanism of interaction (absorption or transmission) and critical stress to DDD
Resume
Dislocation – triple junction
HotQC
Materials?
Perpective

## Slide 31
Thanks for your attention !