## Slide 1: Design and calibration of a 2-cameras characterization prototype
Funding :
Service public de Wallonie | WBGreen Program
Authors : Pierre Barnabé, Godefroid Dislaire, Sophie Leroy, Eric Pirard.
Hyperspectral machine vision applied to recycling

## Slide 2: GeMMe Research Unit

## Slide 3
Introduction
Prototype
Classification
Calibration
Conclusions & Perspectives

## Slide 4: Introduction
Goals:
Classify metallic non ferrous scraps by hyperspectral imaging
Part of a global project dedicated to real-time sorting for industrial application
Context :
Recycling industry needs efficient characterization/sorting tools
European directives for January 2015 : >95% recycling of end-of-life vehicles
Different particle size flows => different approaches

## Slide 5
Prototype
Dispersion system
Conveyor belt
Frame
Specim SWIR Camera
Photonfocus CMOS
with Specim VNIR Spectrograph
Illumination system
Sorting manifold
Cameras
Notes: Superimpose Australia

## Slide 6
Prototype
Frame
Specim SWIR Camera
Photonfous CMOS
with Specim VNIR Spectrograph
Illumination system
Cameras
Translation
Gold coated mirror
Aluminium coated mirror
VNIR
SWIR
Notes: Superimpose Australia

## Slide 7
Prototype
Cameras & mirrors
Notes: Superimpose Australia

## Slide 8: Prototype
Elliptical reflectors :
  Lamp array in one focus
  Measured line in the other focus
Allows to maximise angle of illumination and collected light
Illumination system
Notes: Superimpose Australia

## Slide 9: Classification
Brass
Copper
Zinc
Aluminium
Stainless steel
« Wastes »
+ Lead, magnesium, chromium, iron, cables, glass…
Hand sorted classes (3-15mm)

## Slide 10: Classification
Average reflectance Spectra

## Slide 11: Classification
    PCA
    LDA
Feature extraction

## Slide 12: Classification
LDA + Random Forest classifier results :
Test set : 100 fragments (20 for each class)
Training set : subset of pixels from 5 random fragments by class
Results

## Slide 13: Classification
 |  | Decisions |  |  |  |  | 
 |  | Zinc | Stain. Steel | Copper | Aluminium | Brass | 
True labels | Zinc | 91.1% | 3.2% | 0.2% | 5.1% | 0.3% | 100%
 | St. Steel | 4.3% | 82.0% | 1.4% | 6.2% | 6.2% | 100%
 | Copper | 1.4% | 2.7% | 87.3% | 3.0% | 5.6% | 100%
 | Alu. | 3.0% | 6.1% | 1.0% | 86.6% | 3.2% | 100%
 | Brass | 1.1% | 17.0% | 4.7% | 4.7% | 72.4% | 100%
Pixel level :
Object level :
 |  | Decisions |  |  |  |  | 
 |  | Zinc | Stain. Steel | Copper | Aluminium | Brass | 
True labels | Zinc | 100.0% | 0% | 0% | 0% | 0% | 100%
 | St. Steel | 0% | 100.0% | 0% | 0% | 0% | 100%
 | Copper | 5.3% | 0% | 94.7% | 0% | 0% | 100%
 | Alu. | 0% | 5% | 0% | 95.0% | 0% | 100%
 | Brass | 0% | 9.52% | 0% | 0% | 90.5% | 100%
=> Error = 16.13%
=> Error = 4%
Results : confusion matrix

## Slide 14: Calibration
(Source : www.laserfocusworld.com)
(Imec hyperspectral filter structures)
Spatial direction (line of pixels)
Spectral direction
Sensor
Hyperspectral imaging
  Light Dispersion: transmission or reflective (Offner) diffraction gratings …or even small filters network
  Sensor:
    CMOS/CCD for Visible-and-near-Infrared, 400-1000nm (VNIR)
    Indium gallium arsenide (InGaAs)/Mercury cadmium telluride (MCT) for Short-wavelength-Infrared, 1000-2500nm (SWIR)
  Lens
  Illumination system => Reflectance measurement
Notes: Superimpose Australia

## Slide 15
Calibration
Alignment : Camera & Spectrograph (VNIR)
Notes: Superimpose Australia

## Slide 16: Calibration
Smile Effect (VNIR)
Notes: Superimpose Australia

## Slide 17: Calibration
High pass filter (remove low frequency components)
Find offset between signals from each column and the central column, obtained with maximum of cross-correlation
=> Compute « Smile » vector with offset for each column of the sensor
Smile Effect (VNIR)
Notes: Superimpose Australia

## Slide 18
Calibration
Wavelength & Radiometric Calibration
Wavelength Calibration
Radiometric Calibration
Notes: Superimpose Australia

## Slide 19: Calibration
From signal to reflectance (for a pixel [x,y]):
Where: B = Black reference, pixel x of the line, wavelength i
W= White reference, pixel x of the line, wavelength i
Reflectance presents variations depending of the position of the fragment, his orientation, etc. -> Normalisation to « signatures » (for k wavelengths)
Radiometric Calibration & Reflectance normalization
Notes: Superimpose Australia

## Slide 20
Calibration
Cameras alignment
  Roll, to measure parallel lines (loose fitting screw)
  Pitch, to measure the same line (mirrors orientation)
=> Use of a fine reflectant string
Pixel merging
Geometric calibration for registration
Notes: Superimpose Australia

## Slide 21
Calibration
Pixel merging
  Offsets in spatial pixels and frame number between cameras
Geometric calibration for registration
Notes: Superimpose Australia

## Slide 22: Calibration
Hyperspectral machine vision applied to mineral industry and recycling
Non linearity + Noisy signal
  Depending of the orientation of fragments and hence the actual response of the sensor, reflectance calculated in comparison of the 99% diffuse refl. Spectralon may be biased
  => “Steps” between corrected reflectance of the 2 cameras may appear for a lot of pixels (especially when signal-to-noise ratio decreases)
Combination of halogen light source spectrum
and CMOS response in VNIR
Sensivity of Photonfocus CMOS
Sensibilty of a MCT sensor
(Source : http://www.olympusmicro.com)
Notes: Superimpose Australia

## Slide 23: Calibration
Hyperspectral machine vision applied to mineral industry and recycling
Dynamic noise (moving pattern)
  Delta of subsequent “dark” frames (taken with shutter on) at:
25 FPS
100 FPS
Notes: Superimpose Australia

## Slide 24: Calibration
Hyperspectral machine vision applied to mineral industry and recycling
Dynamic noise (moving pattern)
  Effect visible in noisy bands, for low reflectance objects…
Notes: Superimpose Australia

## Slide 25: Conclusions
  Remarks :
  Monotonous reflectance curves, especially SWIR
  Variability in intensities (depending of orientation)
  Calibration requires attention => before tuning classifiers, optimizing data quality is crucial
+ :
Non destructive
Quick
VNIR is sufficient for most metals => Low cost characterisation tool
- :
Surface properties only!
=> Sample “preparation” (sanding, washing,…) to reduce error
  Limited speed for in-line measurement (need extremely powerful lighting system => problems of heat with halogen)
Lots of data to process

## Slide 26: Thanks for your attention !